Standard PolyDrain – Shallow

Precast Trench Drain 4" ID Shallow depth Channel

Standard Specification

System ID#: PD Shallow 3.1- or PD Shallow 3.9-

Trench drain shall be PolyDrain Shallow; manufactured by ABT, Inc., 259 Murdock Road, Troutman, NC - (800) 438-6057. www.abtdrains.com

System Components:

Precast Trench Drain - The precast trench shall be manufactured using polyester polymer concrete with the following material properties when tested:

Property			    Test Method			Value

Compressive Strength 		    ASTM C579 			14,000 psi Minimum

Bending Strength 		    ASTM C580			4,000 psi Minimum

Tensile Strength 			    ASTM C307			2,000 psi Minimum

Moisture Absorption		    ASTM D570			0.1% Maximum

Chemical Resistance		    ASTM C267 			Pass

Freeze/Thaw w/o weight loss 	    ASTM C666			1,600 Number of Cycles Minimum

Resistance to Fungi 		    ASTM G21			Zero (0) Rating Mold Growth

UL/ULC Listed- Flame Spread 	    UL-723			Class A

The trench consisting of 39.19” (1 meter) channels with nominal 6” (155mm) outside width, 4 “ (100mm) inside width. Channels are non-sloping channels with flat bottoms. Channel depts. Are 3.1” (78.9mm) or 3.9” (99.1mm) as shown on plans. Channels shall have tongue and groove joints. Grate lock down slots shall have polyethylene vibration dampening inserts. All channels must have full length anchoring ribs for a positive mechanical lock with the surrounding concrete.

Frame & Grate: #:  All PolyDrain grates or frame and grates will fit on PolyDrain Channels. Select grate or frame and grate from Standard PolyDrain selections.

Quality Assurance:

Submittals:  A Certificate of Compliance in conformance with the provisions of these Standard Specifications shall be furnished to the Engineer. Grates shall be independently tested to AASHTO M-306.