Standard PolyDrain – 2519CAF

“Incan Myth”

Precast Trench Drain 4" ID w Uncoated Decorative Ductile Iron Grate& Coated Frame

Standard Specification

System ID#: PD 2519CAF Incan Myth

Trench drain shall be PolyDrain; manufactured by ABT, Inc., 259 Murdock Road, Troutman, NC - (800) 438-6057. www.abtdrains.com

System Components:

Precast Trench Drain - The precast trench shall be manufactured using polyester polymer concrete with the following material properties when tested:

Property			    Test Method			Value

Compressive Strength 		    ASTM C579 			14,000 psi Minimum

Bending Strength 		    ASTM C580			4,000 psi Minimum

Tensile Strength 			    ASTM C307			2,000 psi Minimum

Moisture Absorption		    ASTM D570			0.1% Maximum

Chemical Resistance		    ASTM C267 			Pass

Freeze/Thaw w/o weight loss 	    ASTM C666			1600 Number of Cycles Minimum

Resistance to Fungi 		    ASTM G21			Zero (0) Rating Mold Growth

UL/ULC Listed- Flame Spread 	    UL-723			Class A

The trench consisting of 39.19” (1 meter) or 19.56” (1/2 meter) channels with nominal 6” (155mm) outside width, 4 “ (100mm) inside width. Pre-sloped channels shall have a standard slope of 0.6% with radius bottom. Non-sloping channels must have written approval by engineer prior to installation. Channels shall have tongue and groove joints. Grate lock down slots shall have polyethylene vibration dampening inserts. All channels must have full length anchoring ribs for a positive mechanical lock with the surrounding concrete.

Sidewall Extensions – Sidewall extensions for channels may be used for hydraulic performance or to maintain the standard slope of 0.6% in greater trench run lengths. Sidewall extensions shall be composed of similar material and thickness as the channels and shall have tongue and groove joints.

Frame & Grate #2519CAF Incan Myth:  Uncoated ductile iron grate with polymer coated frame conforming to ASTM A-536. Grates shall meet a minimum 494 psi proof load per AASHTO M-306 test modified by utilizing a 9” x 3” load plate and conform to the requirements of the Americans with Disabilities Act Handbook, Section 4.5.4. Frames shall be a minimum of .188” (4.77mm) thick.  The frames shall have .25” dia. x 3” long (minimum) anchors spaced no more than 17” (431.8mm) on center.  Frames shall be independent of the channels. Frames and grates shall seat into channels without rocking and shall be locked to the channel using a zinc plated steel 5/16 – 18 UNC bolt and zinc plated steel toggle bar system with a bolt torque of 10in/lb. Frames and grates shall be made in U.S.A., and shall conform to the FHWA's "Buy America" policy 23 CFR 635.410(b) and Federal Acquisitions Regulations (FAR) 52.225 “Buy American Act”.

Submittals:  A Certificate of Compliance in conformance with the provisions of these Standard Specifications shall be furnished to the Engineer. Grates shall be independently tested to AASHTO M-306.