PDX 6

6” (152mm) ID Precast Trench Drain with High Intake Grate

Standard Specifications

System ID#: PP06-06.502E.FE-F21E

Manufactured by ABT, Inc., 259 Murdock Road, Troutman, NC – (800) 438-6057.  www.abtdrains.com

System Components:

Pre-cast Trench Drain- PP06: The pre-cast trench shall be manufactured using polyester polymer concrete consisting of pre-sloped channels with 6” (152mm) nominal inside width with trapezoidal bottom as shown on the plans. Channels shall be 39.37” (1M) nominal length utilizing tongue and grove connections for channel alignment and sealing. Channel joints shall be sealed with PolySeal II –two part epoxy or equal.

Monolithic polymer concrete shall be made from a composition of aggregate and polyester resin and shall have the following properties when tested as specified below:

Property 			    Test Method			Value

Compressive Strength 		    ASTM C579 			14,000 psi Minimum

Bending Strength 		    	    ASTM C580			4,000 psi Minimum

Tensile Strength 		   	    ASTM C307			2,000 psi Minimum

Moisture Absorption		    ASTM D570			0.1% Maximum

Chemical Resistance		    ASTM C267 			Pass

Freeze/Thaw w/o weight loss 	    ASTM C666			1600 Number of Cycles Minimum

Resistance to Fungi 		    ASTM G21			Zero (0) Rating Mold Growth

UL/ULC Listed- Flame Spread 	    UL-723				Class A

Grating-#06.502E.FE: Black polymer coated ductile iron conforming to ASTM A 536, with a minimum of 0.48Ft2 /L Ft (0.14m2/Lm) open area.  Grates shall meet a minimum 620 psi proof load per AASHTO M-306 test method. Grates must be flush with top of rails.

Frames (Rails)–#F21E: Post fabrication black polymer coated 1.75” x 1.75” x .188” (44.45mm x 44.45mm x 4.76mm) steel angle rails conforming to ASTM A36. Standard headed concrete anchor studs bisect rail-anchoring device a minimum every 12” (305mm).  Grate rails to provide a minimum of 1.187 square inches concrete bearing area per inch of trench length on each side. Grates are retained to frame/rail with appropriate toggle locking device.

Quality Assurance:

Submittals: A Certificate of Compliance in conformance with the provisions of these Standard Specifications shall be furnished to the Engineer.