PDX 12

12” (305mm) ID Precast Trench Drain with ADA Grate

Standard Specifications

System ID#: PP12-12.504G.FB-F21E

Manufactured by ABT, Inc., 259 Murdock Road, Troutman, NC – (800) 438-6057.  www.abtdrains.com

System Components:

Pre-cast Trench Drain- PP12: The pre-cast trench shall be manufactured using polyester polymer concrete consisting of pre-sloped channels with nominal 12” (305mm) inside width with trapezoidal bottom as shown on the plans. Channels shall be 39.37” (1M) nominal length utilizing tongue and grove connections for channel alignment and sealing. Channel joints shall be sealed with PolySeal II –two part epoxy or equal.

Monolithic polymer concrete shall be made from a composition of aggregate and polyester resin and shall have the following properties when tested as specified below:

Property 			    Test Method			Value

Compressive Strength 		    ASTM C579 			14,000 psi Minimum

Bending Strength 		    	    ASTM C580			4,000 psi Minimum

Tensile Strength 		   	    ASTM C307			2,000 psi Minimum

Moisture Absorption		    ASTM D570			0.1% Maximum

Chemical Resistance		    ASTM C267 			Pass

Freeze/Thaw w/o weight loss 	    ASTM C666			1600 Number of Cycles Minimum

Resistance to Fungi 		    ASTM G21			Zero (0) Rating Mold Growth

UL/ULC Listed- Flame Spread 	    UL-723				Class A

Grating-12.504G.FB: Uncoated ductile iron conforming to ASTM A 536-84 with a minimum of 0.25Ft2 /L Ft (0.08m2/Lm) open area.  Grates shall meet a minimum 2496 psi proof load per AASHTO M-306 test. Grates must be flush with top of rails. Grating shall be made in U.S.A., and shall conform to the FHWA's "Buy America" policy 23 CFR 635.410(b) and Federal Acquisitions Regulations (FAR) 52.225 “Buy American Act”.

Frames /Rails–F21E: Post fabrication black polymer coated 1.75” x 1.75” x .188” (44.45mm x 44.45mm x 4.76mm) steel angle rails conforming to ASTM A36. Standard headed concrete anchor studs bisect rail-anchoring device a minimum every 12” (305mm). Grates are retained to frame/rail with appropriate toggle locking device. Frames and retainers shall be made in USA, and shall conform to the FHWA's "Buy America" policy 23 CFR 635.410(b) and Federal Acquisitions Regulations (FAR) 52.225 “Buy American Act”.

Quality Assurance:

Submittals: A Certificate of Compliance in conformance with the provisions of these Standard Specifications shall be furnished to the Engineer. Grates shall be independently tested to AASHTO M-306.

Post Construction Inspection - Grate and grate retainer inspection shall be performed to ensure that all grates and retainers are installed and are properly seated in place.