PDX 5 Interceptor A-69

5” (127mm) ID Precast Trench Drain with High Capacity Grate

Standard Specifications

System ID#: PP05-05.502E.YB

Manufactured by ABT, Inc., 259 Murdock Road, Troutman, NC – (800) 438-6057.  www.abtdrains.com

System Components:

Pre-cast Trench Drain- #PP05: The pre-cast trench shall be manufactured using polyester polymer concrete consisting of pre-sloped channels with 5” (127mm) nominal inside width with trapezoidal bottom as shown on the plans. Channels shall be 39.37” (1M) nominal length utilizing tongue and grove connections for channel alignment and sealing.

Monolithic polymer concrete shall be made from a composition of aggregate and polyester resin and shall have the following properties when tested as specified below:

Property				    Test Method			Value

Compressive Strength 		    ASTM C579 			14,000 psi Minimum

Bending Strength 		    	    ASTM C580			4,000 psi Minimum

Tensile Strength 		   	    ASTM C307			2,000 psi Minimum

Moisture Absorption		    ASTM C570			0.1% Maximum

Chemical Resistance		    ASTM C267 			Pass

Freeze/Thaw w/o weight loss 	    ASTM C666			1600 Number of Cycles Minimum

Resistance to Fungi 		    ASTM G21			Zero (0) Rating Mold Growth

UL/ULC Listed- Flame Spread 	    UL-723				Class A

Frame & Grate: #05.502E.YB:  Uncoated ductile iron conforming to ASTM A-536 with a minimum of 0.28Ft2 /L Ft (.088m2/Lm) open area. Grates shall meet a minimum 620 psi proof load per AASHTO M-306 test modified by utilizing a 9” x 3.75” load plate. The grate and frame assembly shall be independently anchored in the encapsulating concrete. Each 19.69” (0.5m) long grate and frame assembly shall have a minimum anchor flange area of 3.10 in2 (20cm2) per side. Both one and two piece grate and frame assemblies shall withstand a minimum vertical pull out of 1,000 lbs. with a minimum 3,000 psi concrete encapsulation. When a combination of one-piece frame and grates, removable grates with frame, and/or pedestrian safe grates are used; the locations of the grates shall be shown on the plans. Removable grates shall be retained in their frame per manufactures recommendation. The grate retaining devices shall not obstruct hydraulic flow in the channel. All grates shall be bicycle safe. Frames and grates shall be made in U.S.A., and shall conform to the FHWA's "Buy America" policy 23 CFR 635.410(b) and Federal Acquisitions Regulations (FAR) 52.225 “Buy American Act”.

Quality Assurance:

Submittals: A Certificate of Compliance in conformance with the provisions of these Standard Specifications shall be furnished to the Engineer. Grates shall be independently tested to AASHTO M-306.