TFX 8

8” (203mm) ID Trench Forming System with Longitudinal ADA Slotted Grate

Standard Specifications

System ID#: TR08-08.504E.FE-F21E

Manufactured by ABT, Inc., 259 Murdock Road, Troutman, NC – (800) 438-6057.  www.abtdrains.com

System Components:

Forms –TR08: Pre-manufactured trench forms using non-CFC EPS foam.  Forms to be 8.25” (209mm) wide pre-sloped or non-sloped form segments. Each segment to have a full length deforming groove. Non-sloping sections must have written approval by engineer prior to installation.  Forms to have radius bottom and 10.25” (260mm) grate seat width.  Forms to be within .0625” (1.58mm) tolerances.  Invert slope is as noted on plans.  Non-petroleum based form release is to be used for smooth interior walls and easy form removal.

Grating-08.504E.FE:  Black polymer coated ductile iron conforming to ASTM A 536-84 longitudinally slotted with a minimum of 0.39Ft2 /L Ft (0.12m2/Lm) open area and conform to the requirements of the Americans with Disabilities Act Handbook, Section 4.5.4.  Grates shall meet a minimum 620 psi proof load per AASHTO M-306 test. Grates must be flush with top of rails. Grating shall be made in USA, and shall conform to the “Buy America” policy if Federal Aid finances apply.

Frames /Rails–F21E: Post fabrication black polymer coated 1.75” x 1.75” x .188” (44.45mm x 44.45mm x 4.76mm) steel angle rails conforming to ASTM A36. Standard headed concrete anchor studs bisect rail-anchoring device a minimum every 12” (305mm).  Grate rails to provide a minimum of 1.187 square inches concrete bearing area per inch of trench length on each side.  Grates are retained to frame/rail with appropriate toggle locking device.

Quality Assurance:

Submittals: A Certificate of Compliance in conformance with the provisions of these Standard Specifications shall be furnished to the Engineer.

Post Construction Inspection - Formwork is to be fully removed, without exception, to allow for inspection and if needed repair of any voids and or concrete consolidation issues below the frame, trench walls and invert.